Supporting information

Figure S1. The structural and surface characterization of sediment

Figure S2. The structural and surface characterization of humus

Figure S3. The structural and surface characterization of biochar

AMImage size:480 x 360Mag:500xHV:15.0kV

Figure S4. The structural and surface characterization of activated carbon

| Table S1. | Desorption parameters for the PeCB contaminated sediment amended with carbon rich sorbent |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Activated carbon |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | 0.50% |  |  |  |  | 1.00% |  |  |  |  | 5.00% |  |  |  |  | 10.00% |  |  |  |
|  | 14 day | 30 day | 90 day | 180 day |  | 14 day | 30 day | 90 day | 180 day |  | 14 day | 30 day | 90 day | 180 day |  | 14 day | 30 day | 90 day | 180 day |
| Ffast | 6.55% | 1.27% | 100% | 2.52% |  | 3.49% | 0.05% | 2.09% | 0.00% |  | 0.09% | 4.21% | 0.00% | 0.68% |  | 0.44% | 1.34% | 0.00% | 0.10% |
| Fslow | 92.9% | 98.9% | 0.00% | 97.5% |  | 96.5% | 100% | 98.1% | 100% |  | 99.9% | 96.3% | 100% | 99.3% |  | 99.6% | 98.7% | 100% | 99.9% |
| kfast (h-1) | 0.11825 | 0.0897 | 0.00012 | 0.0066 |  | 0.17166 | 0.04267 | 0.000143 | 0.05746 |  | 0.0628 | 0.15109 | 0.06318 | 0.0048 |  | 0.30658 | 0.03223 | 0.03774 | 0.01992 |
| kslow (h-1) | 0.00004 | 0.00004 | 0.00009 | 0.00018 |  | 0.00002 | 0.00010 | 0.00014 | 0.000082 |  | 0.00002 | 0.00008 | 0.000012 | 0.000005 |  | 0.000215 | 0.00062 | 0.000037 | 0.00021 |
| R2 | 0.934 | 0.872 | 0.368 | 0.941 |  | 0.980 | 0.946 | 0.693 | 0.948 |  | 0.879 | 0.638 | 0.742 | 0.882 |  | 0.918 | 0.880 | 0.742 | 0.747 |
|  | Biochar |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | 0.50% |  |  |  |  | 1.00% |  |  |  |  | 5.00% |  |  |  |  | 10.00% |  |  |  |
|  | 14 day | 30 day | 90 day | 180 day |  | 14 day | 30 day | 90 day | 180 day |  | 14 day | 30 day | 90 day | 180 day |  | 14 day | 30 day | 90 day | 180 day |
| Ffast | 72.1% | 1.76% | 0.01% | 14.4% |  | 7.97% | 0.89% | 42.3% | 4.45% |  | 46.0% | 0.72% | 29.4% | 18.0% |  | 20.9% | 0.60% | 71.9% | 7.92% |
| Fslow | 21.2% | 98.3% | 100% | 85.4% |  | 92.5% | 99.1% | 58.1% | 95.6% |  | 50.9% | 99.3% | 71.1% | 83.0% |  | 78.4% | 99.4% | 28.8% | 92.3% |
| kfast (h-1) | 0.16324 | 0.16694 | 0.00034 | 0.00203 |  | 0.10801 | 0.38981 | 0.00047 | 0.01637 |  | 0.10245 | 5.23059 | 0.000416 | 0.01518 |  | 0.000184 | 0.02002 | 0.00056 | 0.0067 |
| kslow (h-1) | 0.00071 | 0.00003 | 0.00034 | 0.00045 |  | 0.00002 | 0.00001 | 0.00047 | 0.00025 |  | 0.00003 | 0.0005 | 0.00041 | 0.000074 |  | 0.000184 | 0.00012 | 0.0006 | 0.0005 |
| R2 | 0.905 | 0.880 | 0.842 | 0.974 |  | 0.952 | 0.933 | 0.904 | 0.974 |  | 0.938 | 0.998 | 0.813 | 0.831 |  | 0.611 | 0.749 | 0.801 | 0.910 |
|  | Hummus |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | 0.50% |  |  |  |  | 1.00% |  |  |  |  | 5.00% |  |  |  |  | 10.00% |  |  |  |
|  | 14 day | 30 day | 90 day | 180 day |  | 14 day | 30 day | 90 day | 180 day |  | 14 day | 30 day | 90 day | 180 day |  | 14 day | 30 day | 90 day | 180 day |
| Ffast | 54.0% | 3.91% | 49.9% | 1.35% |  | 56.8% | 2.07% | 100% | 2.30% |  | 32.7% | 9.80% | 100% | 2.22% |  | 12.6% | 1.59% | 100% | 5.54% |
| Fslow | 42.1% | 96.4% | 50.6% | 98.8% |  | 44.8% | 98.0% | 0.00% | 97.9% |  | 68.1% | 91.4% | 0.00% | 97.9% |  | 87.5% | 98.6% | 0.00% | 94.7% |
| kfast (h-1) | 0.26549 | 0.14583 | 0.00039 | 0.22443 |  | 0.2224 | 0.10948 | 0.00025 | 0.15288 |  | 0.39457 | 0.15556 | 0.000332 | 0.11573 |  | 0.75763 | 0.12568 | 0.000313 | 0.01422 |
| kslow (h-1) | 0.000729 | 0.000026 | 0.000393 | 0.000152 |  | 0.000038 | 0.00011 | 0.000024 | 0.00017555 |  | 0.000087 | 0.000215 | 0.0005121 | 0.0001569 |  | 0.0000007 | 0.000066 | 0.000521 | 0.00036 |
| R2 | 0.884 | 0.795 | 0.839 | 0.919 |  | 0.956 | 0.888 | 0.841 | 0.929 |  | 0.950 | 0.653 | 0.836 | 0.964 |  | 0.996 | 0.720 | 0.808 | 0.982 |