Dear Editor,

We would like to thank You and Reviewers for suggestions. According to Reviewers’ comments, Manuscript was corrected and all required changes in Revised Manuscript II are marked with red color. Responses to Reviewers’ comments are given in the following text:

1. Authors should correct and correctly write following reference:
Yilgör, I.; McGrath, J. E. Polysiloxane Containing Copolymers: A Survey of Recent Developments. Adv. Polym. Sci. 1988, 86, 1.

Reference was corrected.

2. I suggest that authors add Mn of both siloxane precursors (because it is important), regardless that both siloxane reactants are commercially available products, but I leave it to Editor decision.

Values of Mn were given in text now.

3. I suggest that the authors check formula for determination of swelling degree and crosslinking density of siloxane elastomers. I suggest that authors add sweeling degree instead gel content and check crosslinking density calculation. Authors should see some manuscripts concerning calculation swelling degree and crosslinking density, for example:

- J. V. Džunuzović, M. V. Pergal, S. Jovanović, V. Vodnik, „Synthesis and swelling behavior of polyurethane networks based on hyperbranched polymer“, Hem. Ind., 65 (6) 637-644 (2011).
- J.M. V. Pergal, J. V. Džunuzović, R. Poręba, M. Steinhart, M. M. Pergal, V. V. Vodnik, M. Špírková, „Structure-property correlation study of novel poly(urethane-ester-siloxane) networks“, Ind. Eng. Chem. Res., 52 (18) (2013) 6164-6176.

Formula for determination of swelling degree was used from the literature, and authors put new results of equilibrium swelling degree and citied mentioned papers.