Aleksandra Jelić

Innovation Centre, Faculty of Technology and Metallurgy

University of Belgrade

Karnegijeva 4

11120 Belgrade, Serbia

Tel./Fax: +38169604150

E-mail address: jelicalexandra@gmail.com

Editor-in Chief:

Prof. Bojana Obradovič

Faculty of Technology and Metallurgy

Karnegijeva 4

11120 Belgrade, Serbia

Tel: +3811133704

June, 15 2020

Dear Dr. Obradović,

I am pleased to submit the manuscript named “MICROMECHANICAL ANALYSIS OF FATIGUE AND CRACK GROWTH IN CARBON-FIBER EPOXY COMPOSITE MATERIALS BASED ON MECHANICAL TESTING” by Aleksandra Jelić, Milica Sekulić, Marina Stamenović, Vukašin Ugrinović, and Slaviša Putić for consideration for publication as an original scientific paper in the Hemijska industrija (Chemical Industry).

In this study, carbon fibers were used for epoxy resin reinforcement. Samples were derived from a prepreg with specific density of 1600kg/m3. A comparison was done between the fatigue behavior of of crossply (0º/90º) and angleply unnotched and notched carbon/epoxy laminates. Scanning electron microscopy (SEM) study was carried out to determine the pathways that occurred during stress, exhaustion and crack development. The failure of long-fiber reinforced composite laminates was distinguished by the formation and development of many forms of defects: matrix cracks along the fibers, usually in off-axis plies, delamination between neighboring plies and fiber splits. We believe that these findings and the obtained results will be of interest to the readers of your journal.

We declare that this manuscript is original, has not been published before and is not currently being considered for publication elsewhere, and will not be submitted elsewhere while in the reviewing process in the journal Hemijska industrija. If accepted, it will not be published elsewhere including electronically, in the same form, in English or in any other language, without the written consent statement of the copyright-holder.

As a corresponding author, I confirm that the manuscript has been read and approved for submission by all the named authors along with the order of the listed authors. There are no other persons who satisfied the criteria for authorship but are not listed.

The authors have no conflicts of interest to declare. The submitted paper is ethically and professionally correct in every other sense regarding the publishing process.

Three potential reviewers that the authors would like to suggest are:

- Dr Dimitrios Tzetzis, International Hellenic University, School of Science and Technology (d.tzetzis@ihu.edu.gr)

- Dr Guogang Ren, Associate Professor in University of Hertfordshire (g.g.ren@herts.ac.uk)

- Dr Paul Hogg, Professor in Royal Hollow University, (paul.hogg@rhul.ac.uk)

The Corresponding Author is responsible for communicating with the other authors about all parts of publishing process and progress, submissions of revisions and final approval of proofs.

We hope you find our manuscript suitable for publication and look forward to hearing from you in due course.

Sincerely,

Aleksandra Jelić,

Innovation Centre, Faculty of Technology and Metallurgy

University of Belgrade

Karnegijeva 4

11120 Belgrade, Serbia

Tel./Fax: +38169604150

E-mail address: jelicalexandra@gmail.com